## Slide 1: Trouble Shooting for Injection Molding Process

## Slide 2: Type of trouble shooting in injection moulding machine
Black spots
Description:-Black spots appears as a dark spots in the mould part are usually caused by thermal damage to the melt.
Possible solution:-
Decrease the melt temperature.
Decrease the overall cycle time.
clean the screw and barrel.
Decrease the screw speed. High screw speeds may cause the material to degrade.
Material may have too much regrind content.

## Slide 3
Blister
Description:- Blisters are hollows created on or in the mould part. In contrast to avoid this entrapped gas also appear near the walls.
Possible Solutions:-
Decrease melt temperature.
Decrease screw speed.
Dry material.
Increase back pressure.
Increase mold temperature.

## Slide 4: Brittleness
Description:-Brittleness is a condition where the part cracks or breaks at a much lower stress level than would normally be expected based on the virgin material properties.
Possible solution:-
Check for material.
Decrease amount of regrind use.
Decrease back pressure.
Decrease injection pressure.
Increase melt temperature.

## Slide 5: Bubbles
Description:-Bubbles are similar to blisters in that there is air entrapped in the molded part.
Possible solution:-
Decrease injection speed.
Decrease injection temperature.
Dry material further.
Increase injection pressure.
Increase number and/or size of vents.

## Slide 6: Material Leakage
Description:- Material Leakage is usually caused by material forces overcoming the structural strength of the mold.
Possible solution:-
Manifold locator is oversize.
Processing temperature may be too low causing increased pressure in the manifold.
Manifold locator may be hobbed into the mold. Decrease the force applied to the nozzle pad by the machine then repair the damaged area, then check and if necessary replace the locator.

## Slide 7: Excessive Flash
Description:- Excessive Flash is often seen near sealing faces, out of vent or down ejector pins. It appears as thin or sometimes thick sections of plastic where it would not be on a normal part.
Possible solutuion:-
Decrease back pressure.
Decrease cylinder temperature.
Decrease injection hold time.
Decrease injection pressure.
Decrease injection speed.